## Slide 1
NAME
•
POSITION

## Slide 2
INK CHEMISTRY
What are water-based inks?
A stable water-borne system where solids, resins, surfactants and additives work together.
WATER-BASED INK
A stable dispersion in water of very small solid particles in a resinous vehicle, supported by surfactants and other performance additives.
WATER + RESIN + PIGMENT + ADDITIVES = CONTROLLED PRINT PERFORMANCE

## Slide 3
INK CHEMISTRY
What is ink made of?
Every ingredient has a role. The performance comes from how those parts work together.
RESIN / VEHICLE
Creates the system and drives adhesion, resistance and printability.
PIGMENT
The colorant. Grade and shade influence strength, appearance and cost.
ADDITIVES
Fine-tune rub, transfer, foam control, wetting and other performance.
SOLVENTS / VOLATILES
Water is the primary solvent; alcohol can help accelerate drying.
EVERY COMPONENT HAS A JOB. BALANCE THEM FOR CONSISTENT PRINT.

## Slide 4
INK CHEMISTRY
Resin sets the foundation
The vehicle system dictates the primary properties of a printing ink.
RESIN / VEHICLE / EXTENDER
The system dictates the primary properties of a printing ink: • Product resistance • Adhesion • Printability • Ink transfer from system → anilox → plate → board
THE VEHICLE CARRIES THE COLOR — AND SETS THE RULES FOR PERFORMANCE.

## Slide 5
INK CHEMISTRY
Pigment defines the color
Pigment may be dry powder or pre-dispersed. It is often the most expensive raw-material portion of an ink.
WHAT YOU NEED TO KNOW
• Many different grades and shades are available. • Pigment choice changes strength, shade and durability. • Performance demands drive raw-material cost. GENERAL RULE: The more you want the pigment to do, the more expensive it — and the ink — will be.
PIGMENT DRIVES COLOR. PERFORMANCE REQUIREMENTS DRIVE COST.

## Slide 6
INK CHEMISTRY
Additives fine-tune the system
Waxes, transfer aids, defoamer, surfactants, silicone and specialty performance aids enhance the ink system.
COMMON ADDITIVE FAMILIES
• Waxes • Transfer aids • Defoamer • Surfactants • Silicone and specialty performance aids
WHAT THEY CAN IMPROVE
• Rub resistance • Printability • Adhesion • Foam control • Wetting and transfer MORE IS NOT BETTER — use only what the system needs.
USE ADDITIVES WITH PURPOSE — NOT BY HABIT.

## Slide 7
INK CHEMISTRY
Solvents & volatiles
In water-based ink, water is the primary solvent. Alcohol can be used to accelerate drying speed.
60%
WATER / AMINES Provide solubility and re-solubility.
40%
SOLIDS Pigment, polymer and/or filler.
Alcohol may be used as a drying-speed modifier.
CONTROL VOLATILES. CONTROL FLOW, DRYING AND RESOLUBILITY.

## Slide 8
INK CHEMISTRY
Typical water-based ink or coating
A practical way to think about the system: roughly 60% water/amines and 40% solids.
Chart: 
| Water / Amines | Solids
Mix | 60 | 40
60% WATER / AMINES
40% SOLIDS
PIGMENT
Colorant
POLYMER / RESIN
Film formation
FILLER
Performance / cost
SOLIDS = combinations of pigment, polymer and/or filler.
KNOW WHAT IS IN THE MIX — THEN CONTROL WHAT CHANGES ON PRESS.

## Slide 9
pH CONTROL
UNDERSTANDING
pH
pH is a chemistry-control tool — not just a number.
THE pH SCALE
0 ACIDIC
7 NEUTRAL
14 ALKALINE
8.5 – 9.5
FLEXO INKS
TOO LOW
Fast drying • instability • color drift
ON TARGET
Stable chemistry • repeatable performance
TOO HIGH
Slow drying • soft film • odor concerns
GET THE pH RIGHT. GET THE PERFORMANCE RIGHT.

## Slide 10
PH CONTROL
How critical is pH control?
pH drift can create visible ink failure before the operator realizes chemistry has changed.
COLOR
Unstable color / burnout
TRANSFER
Harder to rewet and transfer
CLEANUP
Plate & anilox cleanup gets harder
VISCOSITY
Viscosity can drift with pH
CHEMISTRY DRIFT SHOWS UP AS PRINT DRIFT.
MEASURE EARLY. CORRECT SMALL CHANGES BEFORE THEY BECOME PRESS PROBLEMS.

## Slide 11
PH CONTROL
What pushes pH off target?
Pressroom conditions can quietly destabilize ink chemistry during a run.
1
HEAT + LOW HUMIDITY
Heat and dry air accelerate water and amine loss.
2
DOCTOR BLADE SHEAR
Friction and mechanical energy add heat to the system.
3
OVER-AGITATION
Excessive mixing can accelerate chemistry changes.
4
UNCOVERED INK KITS
Open systems lose volatile components faster.
CONTROL THE ENVIRONMENT AROUND THE INK — NOT JUST THE INK ITSELF.

## Slide 12
PH CONTROL
Low pH creates fast trouble
When pH drops below the control range, stability falls and the system can dry too fast.
LOW pH < 8.8
FAST DRYING LESS STABILITY HARDER REWET
Dries too fast
on anilox, plates or linerboard
1
Less stable
on press
2
Difficult to rewet
on plate
3
Unstable color
shade can move
4
Harder cleanup
resin can stick
5
Viscosity rises
resin can "kick out"
6
LOW pH = LESS CONTROL, MORE STOPS, MORE CLEANUP.

## Slide 13
PH CONTROL
High pH slows the system down
Too much alkalinity can create slow drying, soft film and odor-related problems.
HIGH pH > 9.6
SLOW DRYING SOFTER FILM ODOR RISK
Slower drying
ink stays open longer
Softer film
reduced film strength
Color burnout
appearance can flatten
Viscosity decreases
flow can become too loose
Odor problems
excess amine / alkalinity
Upper-end risk
avoid running at the edge
HIGH pH TRADES DRYING SPEED AND FILM STRENGTH FOR EXCESS ALKALINITY.

## Slide 14
PH CONTROL
Correct pH keeps the press moving
Balanced chemistry supports re-solubility, easier cleanup, stable viscosity and stable color.
CORRECT pH
8.8 – 9.6
TARGET THE MIDDLE — NOT THE EDGES.
GOOD RESOLUBILITY
on plates & roller
FEWER WASH STOPS
more uptime
EASY CLEANUP
less labor
STABLE VISCOSITY
repeatable transfer
STABLE COLOR
more consistent results
STABLE pH → STABLE VISCOSITY → STABLE COLOR.

## Slide 15
PH CONTROL
Take care of pH. Save time and money.
Small chemistry habits compound into meaningful pressroom savings.
1
CLEANUP GETS EASIER
Plate and anilox cleanup is much easier.
2
SHELF INK STAYS USABLE
Ink on the shelf doesn’t come back as mud.
3
RESTORE AT BOTH ENDS
Restore pH at the end of the run as well as the beginning.
4
SAVE TIME + MONEY
Every avoided stop and cleanup adds up.
GOOD pH CONTROL IS PROCESS CONTROL — AND PROCESS CONTROL PAYS.

## Slide 16
VISCOSITY
Viscosity is resistance to flow
The higher the viscosity, the less easily ink flows — and an ink’s pH influences its viscosity.
FLOW
A measure of a liquid’s ability to resist flow. Running viscosity affects how much ink is transferred to the stock.
HIGHER VISCOSITY
More resistance to flow
TARGET VISCOSITY
Balanced flow + transfer
LOWER VISCOSITY
Less resistance to flow
FLOW CHANGES TRANSFER. TRANSFER CHANGES PRINT.

## Slide 17
VISCOSITY
High vs. low viscosity
Running viscosity changes ink transfer, drying and print strength.
HIGH VISCOSITY
• Excess ink transfer • Tracking • Smudging • Slow drying
LOW VISCOSITY
• Weaker print • Dries too fast • Foaming • Poor coverage
TARGET VISCOSITY GIVES YOU CONTROLLED INK TRANSFER, DRYING AND COVERAGE.

## Slide 18
VISCOSITY
Viscosity changes the color you see
Ink transfer changes with viscosity — even when the formula itself does not.
LOW VISCOSITY
Less ink transfer
WEAKER / LIGHTER
Viscosity changes transfer → transfer changes apparent color strength.
STANDARD VISCOSITY
Balanced ink transfer
TARGET COLOR
Viscosity changes transfer → transfer changes apparent color strength.
HIGH VISCOSITY
More ink transfer
DARKER / HEAVIER
Viscosity changes transfer → transfer changes apparent color strength.
SAME INK. DIFFERENT VISCOSITY. DIFFERENT COLOR RESULT.

## Slide 19
PROCESS CONTROL
Build a repeatable control routine
Document checks. Restore chemistry. Repeat at a consistent cadence.
1
BEFORE JOB
Check / restore pH and viscosity before starting a new job.
2
EVERY 30 MIN
Check pH and viscosity throughout the run.
3
END OF RUN
Restore pH at the end of the run.
4
DOCUMENT
Record the checks so trends become visible.
CONSISTENCY COMES FROM A ROUTINE YOU CAN REPEAT — AND VERIFY.
CHECK IT. RECORD IT. RESTORE IT. REPEAT IT.

## Slide 20
PROCESS CONTROL
Don’t let your ink enter the danger zone
Keep pH away from both the lower and higher ends of the acceptable operating range.
WORKING CONTROL RANGE
LOW DANGER
8.8 — 9.6
HIGH DANGER
✓
RUN IN THE MIDDLE OF THE RANGE
Avoid operating near either edge. The closer you get to the limits, the less margin you have for normal pressroom drift.
PROTECT THE MIDDLE. PROTECT THE PROCESS.

## Slide 21
NAME
TITLE | J.M. Fry Inks
✉
☎
EMAIL
PHONE